## Slide 1: Laser Cleaning
MALAMA project lectures
Nikhil Kamboj, Postdoctoral Researcher
Heidi Piili, Adjunct Professor
Eetu Valtonen, Research Assistant
Department of Mechanical and Materials Engineering

## Slide 2: Laser Cleaning
Laser cleaning is a complex physicochemical process
Green, environmentally friendly, and has efficient features
It will gradually replace the traditional cleaning processes such as mechanical, chemical, and ultrasonic
Three methods of laser cleaning process:
  laser dry cleaning
  liquid-assisted laser cleaning
  laser shock wave cleaning

## Slide 3: Traditional cleaning methods and issues
Methods
  Sand blasting
  Chemical solutions
  Shot blasting
  Hydro blasting
2. Issues
  Health and safety
  Consumables
  Logistics
  Waste
  Environment

## Slide 4: Timeline for laser cleaning technology
Integration of laser cleaning and welding
The birth of laser steam cleaning technology
Laser cleaning was 1st time applied to cultural relics preservation
The 1st commercial laser designed for paint stripping of large aircraft
The birth of laser cleaning technology
Laser cleaning was used to remove rust and oxide film on metal surface
Laser cleaning was used to optical lenses
Preparation of superhydrophobic surface by laser cleaning process
Application in nuclear industry
The birth of laser shock wave cleaning technology

## Slide 5: Comparison of cleaning techniques
 | Laser cleaning | Chemical cleaning | Mechanical cleaning | Dry ice | Ultrasonic cleaning
Cleaning method | No contact | Chemical contact | Mechanical abrasion | No contact | Chemical and vibration
Damage to the part | No harm | With damage | With damage | No harm | No harm
Efficiency | High | Low | Low | Medium | Medium
Consumables | Electricity | Chemical agent | Abrasive | Dry ice | Special cleaning agent
Effectiveness | Excellent | Medium | Medium | Excellent | Excellent
Precision | High control | Low control | Low control | Low control | Medium control
Environment | No pollution | Contamination | Contamination | No pollution | No pollution
Operational | Easy | Complex | Complex | Easy | Easy

## Slide 6: Pulse laser cleaning
Laser cleaning is done with a variety of mechanisms, mainly including thermal ablation, stress vibration, thermal expansion, evaporation, phase explosion, evaporation pressure, and plasma shock
Depends on the optical penetration depth and thermal diffusion length
It is necessary to select the appropriate laser source
Critical process parameters include laser beam: energy density, wavelength, pulse length, pulse frequency, angle of incidence, etc., to achieve the best cleaning

## Slide 7: Dry laser cleaning mechanism
1
2
3
4
5
6
7
8
1st
Track
2nd
Track
Steam/
plume
Origin of splash
Dirt layer
Base material
Laser beam interaction zone
Heat affected zone
Thermal stress vibrations
Plume
Pulsed laser beam

## Slide 8: Factors influencing dry laser cleaning
Laser intensity
Laser wavelength
Laser pulse length
Laser incidence angle

## Slide 9: Liquid-assisted laser cleaning
Compared with dry laser cleaning, liquid film-assisted cleaning can reduce the thermal effect caused by laser exposure
The central adhesion of microparticles (dirt) on wet surfaces is capillary force and van der Waals force
Force exerted on the particles by the explosive vaporization of water > greater than the adhesion force of the microparticles

## Slide 10: Laser shock wave cleaning
Indirect laser cleaning technology since it uses shock waves
Laser shock cleaning effectively removes organic and inorganic particles
Usually dry, non-contact, and large-area cleaning technology
Advantageous technology for the photosensitive material like silicon wafer when compared to the direct irradiation of the laser since:
  Minimal thermal effect
  Less local stress

## Slide 11: Lasers used in laser cleaning
CO2
M:YAG (M = Er, Nd, Yb)
GaAlAs diode
XeCl
KrF excimer
Nd:Van
Ti:Sa
Fibre laser (YB, Er, Tm)
Notes: Tm on thullium

## Slide 12: Cleaning metal artefacts
Copper
Iron
Silver
Zinc
Lead
Aluminium
Silver artefact cleaning

## Slide 13: Other materials for laser cleaning
Material | Cleaning
Oxide | OK
Resin | OK
Stains | OK
Dirt | OK
Coatings | OK
Painting | OK
Rust
Uranium
Resin
Stains
Coatings
Notes: Resin = hartsi

## Slide 14: Applications and industry
Rust and corrosion removal - Used to remove rust from small machines or materials kept outdoors for a long time
Paint cleaning - It allows to remove paint of all kinds on metal surfaces
Restoration - In the restoration process, laser cleaning has been used with satisfactory results in, for example, stone preservation
Welding cleaning - Preparing the material for welding processing in the steel industry is vital. Laser cleaning systems can be integrated into production lines
Notes: Restoration = entisöinti

## Slide 15: Conclusions
The laser cleaning mechanism is closely related to the laser wavelength
The laser thermal ablation mechanism and the laser thermal stress mechanism are the most common ones
By selecting suitable laser process parameters and the appropriate laser equipment, surface damage can be completely avoided
Laser cleaning has unique advantages in many industrial fields

## Slide 16: References
Marimuthu, Sundar, Hüsein Kürşad Sezer, and Alhaji M. Kamara. "Applications of laser cleaning process in high value manufacturing industries." In Developments in surface contamination and cleaning: applications of cleaning techniques, pp. 251-288. Elsevier, 2019
Bertasa, Moira, and Capucine Korenberg. "Successes and challenges in laser cleaning metal artefacts: A review." Journal of Cultural Heritage 53 (2022): 100-117
Zhu, Guodong, Zhenhai Xu, Yang Jin, Xi Chen, Lijun Yang, Jie Xu, Debin Shan, Yanbin Chen, and Bin Guo. "Mechanism and application of laser cleaning: A review." Optics and Lasers in Engineering 157 (2022): 107130
Salimbeni, Renzo. "Laser techniques for conservation of artworks." Archeometriai Műhely 3, no. 1 (2006): 34-40.

## Slide 17: Precaution note